## Slide 1: 6 and 8 October Photonics-PPT #1 Photovoltaics PPT#2 Will Cover Lighting

## Slide 4
50.0
UV
(FIR)
VIS
NIR
40.0
30.0
20.0
10.0
3.0
2.0
1.5
0.7
0.3
0.4
0.5
0.6
Wave Length (µm)
MIR (3~30 µm)
Part of the Spectrum
Sun
Visible Spectrum From About 0.4 micrometers Blue) to 0.7 micrometers (Red)
UV-Ultraviolet
NIR-Near Infrared or Just IR
MIR and FIR Middle and Far Infrared

## Slide 6: Solar Energy Spectrum
Spectrum of the solar energy
Solar radiation outside the earth’s surface:
1.35 kW/m2, 6500 times larger than world’s energy demand
AM0: radiation above the earth’s atmosphere
AM1.5: radiation at the earth’s surface
Blackbody radiation: ideal radiation

## Slide 8: Operation Principle of Solar Cells

## Slide 9
From EE 2212 Text

## Slide 12
12
12
12
Summary of Loss Mechanisms of Semiconductor Solar cells
Loss
Optical loss
Electrical loss
Heat
hv >EG
No absorption
hv <EG
Reflection
Shadowing
Incomplete absorption
Ohmic
Recombination
SC material
Contact material
Metal-SC
SC surface
SC body
Depletion region
Manufacture defects proving alternate current path
Notes: 12

## Slide 13
13
13
Circuit-Model for Ideal Solar Cell
13
ISC
IDark
RSH
RS
Load
“Ideal” means that the resistive losses are ignored.
ISC
IDark
RSH
RS
Load
IDark
RSH
RS
Notes: 13

## Slide 14
14
14
Circuit-Model for Solar Cell with Resistive Losses
14
ISC
IDark
RSH
RS
Load
RSH: shunt resistance. It accounts for manufacture defects of the material. Low shunt resistance causes power loss by providing additional path for light-generated current.
RS: series resistance. Series resistance in a solar cell has three causes: (1) the movement of current through the emitter (n-type, heavily doped) and base (p-type, moderately doped) of the solar cell; (2) the contact resistance between the metal contact and the silicon; (3) the resistance of the top and rear metal contacts.
Notes: 14

## Slide 15
15
15
Design of High Efficiency Solar Cells
15
Techniques and design features adopted to produce the highest possible efficiencies include:
Very fine metal contact lines, typically less than 20 µm wide, to minimise shading losses;
Small area devices and good metal conductivities, to minimise resistive losses in the metal grid;
Use of elaborate metallization schemes, such as titanium/palladium/silver, that give very low contact resistances;
Good rear surface passivation, to reduce recombination;
Use of anti-reflection coatings, which can reduce surface reflection from 30% to well below 10%.
Use solar concentrator
Notes: 15

## Slide 16: Multi-Junction Semiconductor Solar Cells
16
Feature: split the spectrum and use a solar cell with multiple sections. Each section is optimized to each section of the spectrum.
The top cell absorbs high energy photons.
The bottom cell absorbs low energy photons.
Eg1
Eg2
Eg3
Top layer
Bottom layer
Arrangement of layers based on bandgap.

## Slide 17: Absorption Spectrum of Multi-junction Cells
17
Highest efficiency achieved so far is 46%
Two junction tandem solar cells

## Slide 18: NREL’s Measurement of Best Solar Cell Efficiencies
18

## Slide 19: Work Record for Solar Cells Efficiency at 47.1% by NREL
19
Six-junction III-V solar cell

## Slide 20: Multi-Junction Solar Cell Efficiency at 46%
20

## Slide 21
21
Solar Cell with 44.4% Efficiency by Sharp
III-V compound Semiconductors
Solar concentrator
Triple junction tandem solar cell

## Slide 22
22
22
Multi-bandgap Solar Cells
p+ GaAs (311)B substrate
100 nm p GaAs
100 nm n GaAs
30 nm n GaInP
200 nm n+ GaAs
Au grid bar
Au contact
UD GaAsP
UD GaAsP
UD GaAsP
UD GaAsP
Lattice parameter
0.5 µm intrinsic region
InGaAs QDs
InGaAs QDs
InGaAs QDs
QD Solar Cell design
CB
VB
IB
ECI
EIV
h(ν1+ ν 2)
or hν3
Band structure of QDSC
Feature: additional photon absorption windows in the solar spectrum
Objective: investigate non-radiative transition mechanisms that could degrade the photovoltaic conversion efficiency;
Strategy: build QDSC model to including all possible transition mechanisms

## Slide 23
Plasmonic Solar Cells
H. A. Atwater and A. Polman, Nature Materials, Vol 9, March 2010

## Slide 24: Dye-sensitized Solar Cells (DSSCs)
Electrolyte containing redox couple
Dye-sensitized TiO2 layer
Polymer sealant
Conducting glass plate for the photo-anode
SnO2 layer
Pt layer
Conducting glass plate for the cathode
Feature: easy and cheap fabrication, but low output power

## Slide 25: Perovskite Solar Cells
Features:
(1) Cheaper fabrication cost vs. efficiency achieved, flexible cell structure
(2) Weakness: poor long-term stability, and high heat loss
Source: www.medium.com

## Slide 27
The typical amorphous silicon cell employs a p-i-n design, in which an intrinsic layer is sandwiched between a p layer and an n layer.
Amorphous silicon's random structural characteristics result in deviations like "dangling bonds." Dangling bonds provide places for electrons to recombine with holes, but this may be neutralized somewhat with hydrogen.
http://www.nrel.gov/index.html
).
http://www.powerfilmsolar.com/
http://www.powerfilmsolar.com/education/calculations/

## Slide 29: 5.6 KW Photovoltaic Array (Funding incorporated within the Malosky Stadium Renovation Budget) CIP Grant Through Minnesota Power Provides Funding For Instrumentation and EE Students To Develop A WEB Presence)