## Slide 1: SEMICONDUCTOR DEVICE FABRICATION
AN OVERVIEW
Presented to
EE 2212
Text Section 2.11 Supplement
30 January Through 3 February 2017

## Slide 2: OUTLINE
Dimensions and Units
What is a Monolithic (“Single Stone”) Integrated Circuit (IC)?
Fabrication and Integrated Circuit Overview
Historical Perspectives
Photolithography
Basic process sequence
Packaging
Basic Processing Steps Summary
Other Devices and Technologies

## Slide 3: DIMENSIONS AND UNITS
1 micrometer (1 mm) = 10-6m = 10-4cm
1 Å = 10-10m = 10-8cm (Å =Angstrom)
10,000 Å = 1 mm = 1000 nm
1 nanometer (1 nm) = 10-9 m = 10 Å
Wavelength of visible light 0.4 mm(violet) to 0.7 mm(red)
{400 nm to 700 nm, 4,000 Å to 7,000 Å }
1 mil = 0.001 inch = 25.4 mm
Sheet of notebook paper about 4 mils = 100 mm
1 human hair = 75 mm to 100 mm = 75,000-100,000 nm
Atomic spacing in a crystal ~ 3 to 5 Å
Fingernail growth rate about 1-3 mm/hour (Not personally verified)
Aggressive production minimum feature sizes, tens of nm, 20 nm used in the iPhone 6 A8 microprocessor, 14 nm in state-of-the-art memory from Micron
Speed of Light c= 3x108m/sec = 300 m/μsec = 0.3 m/nsec (About 1 foot/nsec)
3 GHz clock speed
T = 0.33 nsec
Signal or Photon Travels About 4 inches

## Slide 4
4
IC Fabrication Overview
Procedure of Silicon Wafer Production
Raw material ― Polysilicon nuggets purified from sand
Crystal pulling
Si crystal ingot
Slicing into Si wafers using a diamond saw
Final wafer product after polishing, cleaning and inspection
A silicon wafer fabricated with microelectronic circuits
Up to you. Keep in touch.
Up to you. Keep in touch.
Notes: (1) Raw material from sand and made into the polysilicon nuggests
(2) The polysilicon nuggets are placed into the quartz crucible. Quartz crucible, surrounded by graphite heater, 1600degree C. Metling it rotated. The melted nuggets can be pulled out slowly using a crystal seed. The crystal seed the shape is long thin needle. When it pull out and colled and formed the cylinder shpaed inget. The ingot is single crystal slicon.The diameter of the ingot is deciced by the temperature when melting and the rotating speed when it pulled out.
Pure crystal cylindar ingets.temparatue and rate decide the diameter

## Slide 9
Stanley G. Burns
UMD-ECE

## Slide 13
<$40
256 GB
14 nm

## Slide 19: BASIC PROCESSING STEPS Design Then Repeated Application Of:
Oxidation and/or Nitridation
Photolithography
Wet Etching (Chemical)
Dry Etching (Plasma)
Ion Implantation and/or Diffusion
Evaporation
Sputtering
Plasma Assisted Deposition
Epitaxy
Many Processing Steps are at temperatures to 1200°C

## Slide 21: OTHER DEVICES AND TECHNOLOGIES
Thin-Film Transistors (TFT) for displays and cameras
Displays-Liquid Crystal Displays (LCD), Plasma, LED Backlit, etc. Television, computer, and smart phone screens
Photonic-Light Emitting Diodes (LED), Organic Light Emitting Diodes (OLED), LASERS, Optical Chips, etc.), Lighting
Photovoltaics-Conventional Crystalline and Flexible Thin-Film
Devices and Systems on Flexible Substrates. Next generation of smart phones
Micro-Electro-Mechanical Systems (MEMS) integration of mechanical elements, sensors, actuators, and electronics on a common silicon substrate through microfabrication technology. Automotive, medical, personal electronics