## Slide 1
Overview of Sputtering System
Applications (low pressure process)
Thin film deposition
  Metals (DC sputtering)
  Dielectrics: silicon dioxide and aluminum oxide (RF sputtering)
  Alloys (Al-Cu-Si)
  Etching
Sputter yield
Sputtering Technologies
DC (diode) sputtering
RF (radio frequency) sputtering
Magnetron sputtering
Reactive sputtering
18 and 20 October
Deposition Part 2

## Slide 2
Basic Sputtering System
DC or RF

## Slide 4
Mechanisms of Sputtering
Sputtering is a process that atoms are ejected from a solid target material due to bombardment of the target by energetic particles
+
Incident ions
Reflected ions and neutral atoms
Secondary electrons
Sputtered ions from the target material
Surface
Target material
Ions with very low energy may be reflected away from the surface.
Ions with energy less than 10eV, could also be adsorbed to the surface, giving up their energy as heat.
Ions with energy above about 5keV, will penetrate into the material and transfer their energy to atoms in the target material.
Ions with medium energy, transfer part of energy to heat and use the other part of energy for physical rearrangement of the target surface. The atoms of the target materials will be ejected out.

## Slide 5
Sputter Yield
Sputtering process is characterized by sputter yield (S), which is a measure of efficiency of sputtering
Sputter yield depends on:
the energy of incident ions
the mass of incident ions
the mass of target atoms
the binding energy of atoms in the target
the incident angle of ions

## Slide 6
Sputter Yield (Cont’d)
For each target material, there exists a threshold energy, below which no sputtering occurs

## Slide 7
DC and RF Sputtering System
DC or RF
DC sputtering:
Used for sputtering metal materials, such as Al, Ti, and Au. The target acts as the cathode in a diode system
RF sputtering:
Used for dielectric materials, such as SiO2, and Al2O3.
(Using DC sputtering for dielectric material will cause the buildup of positive charges on the target. The alternating potential voltage can avoid the charge buildup)

## Slide 8
Pressure Effect
Compromise between
increasing number of Ar ions
increasing scattering of Ar ions with neutral Ar atoms
Optimal pressure is around 100mTorr
(1Torr =133Pa)
How to increase the number of Ar ions without increasing the pressure?
Magnetron sputtering

## Slide 9
  CVD-Various Techniques
  Atmospheric pressure CVD (APCVD) – CVD at atmospheric pressure
  Low-pressure CVD (LPCVD) – CVD at sub-atmospheric pressures
  Ultrahigh vacuum CVD (UHVCVD) – CVD at very low pressure, typically below 10−6 Pa (~10−8 torr)

## Slide 11
Polysilicon
Polycrystalline silicon is deposited from trichlorosilane (SiHCl3) or silane (SiH4), using the following reactions:[
SiH3Cl → Si + H2 + HCl
SiH4 → Si + 2 H2
Silicon Dioxide
SiH4 + O2 → SiO2 + 2 H2
SiCl2H2 + 2 N2O → SiO2 + 2 N2 + 2 HCl
Si(OC2H5)4 → SiO2 + byproducts
Silicon Nitride
Silicon nitride is often used as an insulator and chemical barrier in manufacturing ICs. The following two reactions deposit silicon nitride from the gas phase:
3 SiH4 + 4 NH3 → Si3N4 + 12 H2
3 SiCl2H2 + 4 NH3 → Si3N4 + 6 HCl + 6 H2
Or to deposit SiNH:
2 SiH4 + N2 → 2 SiNH + 3 H2
SiH4 + NH3 → SiNH + 3 H2
Metals
WF6 → W + 3 F2
WF6 + 3 H2 → W + 6 HF
Similar reactions for Al using triisobutylaluminium (TIBAL) [Organometallic compounds]
Molybdenum, Tantalum, Titanium-Recall we discussed “silicides” earlier this semester.

## Slide 13
A process that uses ions of an inert gas to dislodge atoms from the surface of a crystalline material, the atoms then being electrically deposited to form an extremely thin coating on a glass, metal, plastic, or other surface.

## Slide 14
Designs of Magnetron Sputtering System
SM: solenoid magnet
M: magnet
E: electric field
B: Magnetic field
T: Target
P: Plasma
S: Substrate
Advantages:
Could be used together with DC or RF
Higher sputter efficiency due to the increase of ionization of Ar atoms
  Higher sputter rate under lower pressure (10-5 or 10-3 Torr)
  Increase probability of electrons striking Ar atoms

## Slide 15
Parameters for Magnetron Sputtering
Deposition pressure : 10-5 to 10-3 Torr
  Pressure for DC or RF Sputtering: ~ 0.1 Torr
  Pressure for evaporation: ~ 0.01 Torr
Deposition rate : 0.2 ~ 2 μm/min
  10 times higher than DC or RF sputtering
  Deposition rate for evaporation is 2 ~5 μm/min
Deposition temperature: 100 to 150oC
  Evaporation temperature is above 1000oC

## Slide 16
Reactive Sputtering
Sputtering metallic target in the presence of a reactive gas mixed with inert gas (Ar)
  A mixture of inert +reactive gases used for sputtering
      oxides – Al2O3, SiO2, Ta2O5 (O2)
    nitrides – TaN, TiN, Si3N4 (N2, NH3)
  carbides – TiC, WC, SiC (CH4, C2H4, C3H8)
Chemical reaction takes place on substrate and target
Can poison target if chemical reactions are faster than sputter rate
Adjust reactive gas flow to get good stoichiometry without incorporating excess gas into film

## Slide 17
Comparison between Evaporation and Sputtering
Evaporation | Sputtering
Low energy atoms (~ 0.1 eV) | High energy atoms/ions (10 –20 eV) Better adhesion
Low pressure, high vacuum Directional in nature Lower impurity | Higher pressure for DC/RF, but much lower pressure for magnetron sputtering Poor directional Argon atoms implanted in the film
Poor step coverage | Better step coverage
Point source, poor uniformity | Parallel plate source, better uniformity
For compound materials and alloys, different components evaporate at different rate, which leads to poor stoichiometry | For compound materials, all components sputtered with similar rate, which helps maintain stoichiometry
Physical process | DC, RF, and magnetron sputtering are physical processes Reactive sputtering is chemical process

## Slide 19: Chemical vapor deposition (CVD)
19
      Physics and Chemistry in CVD process
      Atmospheric CVD (APCVD)
      Low pressure CVD (LPCVD)
      Plasma-enhanced CVD (PECVD)
      Metal organic CVD (MOCVD)

## Slide 20
Simple CVD Reactor
Temperature of the susceptor should be maintained, which is more challenging for PECVD system.
Cooling system inside the susceptor in PECVD: plasma discharge increased the susceptor temperature. Cooling is performed by circulating a coolant through a tube inside the susceptor in order to sustain the susceptor temperature for large-area and high rate deposition. (YB Lim, et al., Int. J. Precis. Eng. Man., 13(7), 2012)

## Slide 21
Physics and Chemistry in the Reactor
CVD Process:
Introduce reactive gases to the chamber
Thermal decomposition of the gases through heat or plasma
Gas absorption by substrate surface
Reaction takes place on substrate surface and film is firmed
Transport of volatile byproducts away form substrate
Exhaust waste
Example: SiH4 (g)→ Si (s) +2H2 (g) (for polysilicon)
Physics and chemistry involved:
(1) Dilution of the SiH4
The decomposition of silane gas (SiH4) around the susceptor decreased the deposition rate and concentration of silane along the length of the reactor;
The silane can be mixed with in an inert carrier gas, i.e., H2, to improve the uniformity of deposition;
The surface will have concentration of vacancies brought by H2.
(2) Homogeneous and Heterogeneous reaction
Homogeneous: atoms of the solid are released from the gas (undesired)
Heterogeneous: atoms of the solid form on the wafer surface (preferred)

## Slide 22
Physics and Chemistry in the Reactor (2)
Example: SiH4 (g)→ Si (s) +2H2 (g)
(3) Other reactions in the reactor
SiH4 (g)→ SiH2 (s) +H2 (g)
SiH4 (g)+ SiH2 (g) → Si2H6 (g)
SiH6 (g) → HSi2H3(g)+H2(g)
How to judge which reaction is dominant?
The equilibrium constant for each reaction.
(4) Gas flow:
Gas flow determines the transport of the various chemical species in the chamber
Important for temperature distribution
(5) Temperature effects:
Deposition rate
Uniformity
Hot wall batch CVD reactor: for large batch processes, excellent temperature control, but low deposition rate

## Slide 23
Atmospheric CVD (APCVD)
Features:
High reaction rate, poor uniformity and purity
Run at atmospheric pressure
Used for thick dielectrics with deposition rate higher than 1000Å/min
Example: SiH4 (g) + O2 (g)→ SiO2 (s) +2H2 (g)

## Slide 24
Low Pressure CVD (LPCVD)
Features:
Hot wall system and cold wall systems:
  Hot wall system: uniform temperature distributions, but has deposition on the walls
  Cold wall system: with reduced deposition on the walls
Used for polysilicon and dielectrics (mostly in hot wall systems)
Good purity, low deposition rate than APCVD
Low pressure in the chamber (0.1 to 1.0 Torr)
Temperature 550 ~ 650ºC

## Slide 25
Plasma Enhanced CVD (PECVD)
Features:
Deposit at low substrate temperature
Used to deposit dielectrics over Al or GaAs
Use plasma to enhance the decomposition and reaction in the CVD
Very good at filling small features
May induce plasma damage
Plasma may increase the substrate temperature, so cooling on the substrate is important
  Temperature can be as low as 120ºC

## Slide 26
Metal Organic CVD (MOCVD)
Use gaseous organic precursors
Advantages: highly flexible—> can deposit semiconductors, metals, dielectrics
Disadvantages: highly toxic, very expensive source material, environmental disposal
costs are high.
Uses: dominates low cost optical (but not electronic) III-V technology, some metallization
Features

## Slide 27: Summary on CVD
27
 | APCVD | LPCVD | PECVD | MOCVD
Advantages | High growth rate at atmospheric pressure | Low pressure, high purity | Low temperature Good for filling small features | flexible
Disadvantage | Poor purity | Low growing rate | Plasma damage | Toxic, expensive source materials
Materials | Thick dielectric materials | Poly-Si and dielectric materials | Dielectrics over Al or GaAs | III-V materials

## Slide 28
Epitaxy
What is it: deposition of a crystalline overlayer on a crystalline substrate.
Requirement: the substrate must act as seed crystal with preferred crystal orientation
Application: to deposit single-crystal silicon (30~100 μm), compound semiconductors and semiconductor heterojunctions
Epitaxy methods:
Vapor phase epitaxy (VPE) (very common)
Molecular beam epitaxy (MBE)
Process:
Wafer cleaning: to remove native oxide and any residual impurities and particles
  RCA cleaning procedure: (1) remove organic residues (SC-1); (2) remove thin oxide layer; (3) remove metallic contaminations (SI-2)
Epitaxy growth

## Slide 29
Molecular Beam Epitaxy (MBE)
MBE process:
The crystalline layer is formed by deposition from a thermal beam of atoms or molecules.
Deposition is performed in ultrahigh vacuum conditions (10-10 Torr)
Substrate temperature: 400 ~ 900ºC
Application:
Growth thickness with atomic resolution
Good growth quality for semicondutor heterostructures

## Slide 30
Vapor Phase Epitaxy (VPE) Process
A simple VPE system.
VPE steps:
Gas phase decomposition;
Transport to the surface of the wafer;
At the surface:
(3) Adsorb;
(4) Diffuse;
(5) Decompose
(6) By-product desorb