## Slide 1
Temperature: 900 ~1200 ºC
Two Basic Reactions (Justifications for Each)
Dry oxidation: Si (solid) + O2 (gas) → SiO2
Wet oxidation: Si (solid) + 2H2O (vapor) → SiO2 + 2H2
Growth of SiO2 on Si:
Si is consumed (oxidized) as the oxide thickness increases
The resulting oxide “expands” during growth
The final oxide layer is approximately 54% above the original silicon surface and 46% below the original surface as we will now show
Oxidation Chapter 4
24 and 27 September 2021
  Thermal oxidation process
  Modeling for oxidation
  Factors influencing oxidation rate
  Oxidation systems
  Measurement of silicon dioxide thickness

## Slide 2
  Oxidation System
Oxidant is introduced in gaseous form.
High-impurity O2 is used for dry oxidation
Water vapor is introduced by passing oxygen through a bubbler containing deionized water heated to 95ºC.

## Slide 4
J

## Slide 5
Modeling for Oxidation-Duplicate of Previous Slide
Concentration, N
No
Ni
SiO2
Si
J
Xo
Distance from surface, x
Xo: thickness of the oxide at a given time
No: oxygen concentration at the SiO2 surface (cm-3)
Ni: oxygen concentration at the SiO2-Si interface (cm-3)
J: oxygen flow per unit area, i.e., the flux (cm-2s-1)

## Slide 6
o
o
o
o
o
t
o
o

## Slide 7
Duplicate of Previous Slide
Diffusion equation:
In order for the oxidation to occur, oxygen must reach the SiO2-Si interface.
As the oxide grows, oxygen must pass through more and more oxide, and the growth rate decreases as time goes on
The oxidation model is built upon the diffusion of oxygen through the existing SiO2 layer
Flux is proportional to the oxidizing species:
If M is the volume concentration of molecules of the oxidizing species

## Slide 8
More DFQ Solution Details
With the initial condition:
Solve the differential equation:
The SiO2 at any time t is solved as:
and
For short time with
For long time with
(B/A) is called linear growth rate constant
B is called parabolic rate constant
letting
t is the time taken to grow the additional thickness (Xo-Xi)
The above equation becomes
the solution comes out as:

## Slide 9
  Factors Influencing Oxidation Rate
Temperature
Wet and dry oxidation
Pressure
Crystal orientation
Impurity doping
Pressure: both linear and parabolic rate constants are proportional to No, the oxidant concentration at the top SiO2 surface, and No is proportional to the pressure
Doping: Phosphorus doping increases the linear rate constant without altering the parabolic rate constant. Boron doping increases parabolic rate constant but has little affect on the linear rate constant. This is due to the impurity redistribution during oxidation.

## Slide 11
  Factors Influencing Oxidation Rate (1)
Diffusion coefficient
Unit of D: cm2/sec
Plot of the B oxidation coefficient. The wet parameters depend on the H2O concentration and therefore on the gas flows

## Slide 12
Factors Influencing Oxidation Rate
Temperature:
Plot of the parabolic rate constant B versus temperature.
Plot of the linear growth rate constant B/A versus temperature.

## Slide 13
  Factors Influencing Oxidation Rate (3)
Wet and dry oxidation: water vapor has a much higher solubility than oxygen in SiO2.
Slower growth results in a denser, high-quality oxide.
Crystal orientation: the crystal orientation changes the number of silicon atoms and bonds available at the silicon surface, which influences the oxide growth rate and the quality of Si-SiO2 interface
 | Wet |  | Dry | 
 | D0 (μm/hr) | EA (eV) | Do(μm/hr) | EA(eV)
<100> Silicon | 9.7×107 | 2.05 | 3.71×106 | 2.00
<111> Silicon | 1.63×108 | 2.05 | 6.23×106 | 2.00
Values for Coefficient Do and Activation Energy EA

## Slide 14
Diffusivities Into SiO2

## Slide 21
  Measurement of Silicon Dioxide
Through color of reflected light
Mechanical surface profiler
Ellipsometer
Ellipsometer (Accurion.com)
Stylus profiler (Druker.com)